SECTION 09 84 33 -   SOUND ABSORBING WALL UNITS

GENERAL

Drawings and general provisions of the Contract, including General and Supplementary Conditions and Division 01 Specification Sections, apply to this Section.

SUMMARY

Section Includes:

Custom fabricated acoustical wall panels.

        - Related Sections include the following:

          - Division 01 Section “Construction Waste Management”

          - Division 09 Section, "Acoustical Space Units Sound Diffusers and Reflectors"

REFERENCES

ASTM International:

ASTM C423 Standard Test Method for Sound Absorption and Sound Absorption Coefficients by the Reverberation Room Method.

ASTM E84 Standard Test Method for Surface Burning Characteristics of Building Materials.

ASTM E795 Standard Practices for Mounting Test Specimens During Sound Absorption Tests.

SYSTEM DESCRIPTION

Performance Requirements:

Surface Burning Characteristics (ASTM E84):

Flamespread: 25 maximum.

Smoke Developed: 250 maximum.

SUBMITTALS

General: Submit listed submittals in accordance with Conditions of the Contract and Division 01 Submittal Procedures Section.

Product Data: Submit product data sheet, for specified products.

Shop Drawings: Submit shop drawings showing layout, edge profiles and panel components, including anchorage, accessories, finish colors and textures.

Samples: Submit selection and verification samples of finishes, colors and textures.

Test Reports: Certified test reports showing compliance with specified performance requirements.

Standard Systems: Submit certified copies of previous test reports substantiating performance of system in lieu of retesting.

DELIVERY, STORAGE & HANDLING

General: Comply with Division 01 Product Requirements Section.

Delivery: Deliver materials in manufacturer’s original, unopened, undamaged containers with identification labels intact.

Storage and Protection: Store materials protected from exposure to harmful environmental conditions and at temperature and humidity conditions recommended by the manufacturer.

PROJECT CONDITIONS

A.	Temperatures

1.	Maintain substrate surface and ambient temperatures above 55 degrees F, unless required otherwise by manufacturer’s instructions.

2.	Do not apply adhesive when substrate surface temperature or ambient temperature is below 55 degrees F.

3.	Maintain these conditions 72 hours before, during, and after installation of vinyl wallcovering.

B.	Lighting: Provide not less than 80 foot candles per square foot minimum, measured mid- height on the surfaces to receive wallcoverings.

- Wall Condition

- The wall surface should be clean, dry, structurally sound, and free of mildew, grease, dust, or other stains.

- Remove any existing wallcovering and adhesive.

- Plaster and masonry wall surfaces should not exceed 5.5% moisture when measured by a BD-8 Delmhorst moisture meter.  Gypsum board wall surfaces should not exceed 16% moisture.

- Room humidity should not exceed 90%.

- Wall surfaces should be primed with a quality wallcovering primer as approved by manufacturer.  Wall surfaces with significant color variation should be primed with a good quality pigmented wallcovering primer.

- New plaster should age 60-90 days before painting or installing wallcovering.

PRODUCTS

ACOUSTICAL WALL PANELS

Manufacturer: Zintra Acoustic Solution

All Acoustical Wall Panels shall be the product of one distributor.

Acoustical Wall Panels shall be __________ as distributed by MDC, Glendale Heights, IL www.mdcwall.com.  Contact 800-621-4006

MANUFACTURED UNITS

Zintra Acoustic Textiles Panels:

Constructed using Polyester Fiber

Thickness: 12mm (0.47”)

Size: As indicated on the drawings up to a maximum 48 inch (1219 mm) x 108 inch (2743mm) panel.

Edge Detail: [Square]

Sound Absorption (ASTM C423): Noise Reduction Coefficient as follows:

1/2 inch (12.7 mm) Panel: 0.45, minimum.

Mounting Accessories: [Neutral Cure Silicone Adhesive] [Z-clips]

Zintra on Zintra Acoustic Panels

Constructed: Perforated Polyester fiber panel bonded to another sheet of polyester fiber

Thickness: [24mm (0.95”)]

Size: As indicated on the drawings up to a maximum 48 inch (1219 mm) x 108 inch (2743mm) panel.

Edge Detail: [Square]

Sound Absorption (ASTM C423): Noise Reduction Coefficient as follows:

1/2 inch (12.7 mm) Panel: 0.75, minimum.

Mounting Accessories: [Neutral Cure Silicone Adhesive] [Z-clips]

FABRICATION

General: Utility knife, panel saw or oscillating knife on CNC machine

EXECUTION

CONSTRUCTION WASTE MANAGEMENT

The contractor, subcontractors, and their personnel shall follow the procedures and practices for waste separation, collection and transport as defined in the contractor’s “Waste Management Plan” as required by Division 01 Section "Construction Waste Management."

MANUFACTURER’S INSTRUCTIONS

Compliance: Comply with manufacturer’s product data, including product technical bulletins, product catalog installation instructions and product carton instructions for installation.

EXAMINATION

Site Verification of Conditions: Verify that substrate or supporting structure, which has been previously installed under other sections, is acceptable for product installation in accordance with manufacturer’s instructions.

Hard Side:

Verify that stud spacing is 16 inches (406 mm) on center, maximum, for panels installed over open studs.

Do not install panels until unsatisfactory conditions are corrected.

CLEANING

Follow manufacturer’s instructions for cleaning panels soiled during installation. Replace panels that cannot be cleaned to as new condition.

Keep site free from accumulation of waste and debris.

END OF SECTION 09 84 33